## Slide 1: Evaluating the wettability and dynamic water absorption of textiles
Yuyang Wang

## Slide 2
Wettability
Introduction
Methodology
Results and analyses
Conclusion
Experiments
Fabrics and apparatus design
Downward infiltration
Lateral and upward infiltration

## Slide 3: Importance of the dynamic water absorption and wicking behavior
The dynamic water absorption and wicking behaviour is an important index to evaluate the comfort of clothing garments;
The liquid transfer property can assess the internal structures and porosities of textiles;

## Slide 4: Current ways to test the infiltration process
Liquid-dropping method
http://www.scienceknowledge.org/2010/02/22/german-researchers-develop-miracle-material/
http://sbifinishing.com/services/water-resistance/

## Slide 5: Current ways to test the infiltration process
Wicking height method
http://www.tikp.co.uk/knowledge/material-functionality/hydrophilicity/wicking/?print=true

## Slide 6: Current ways to test the infiltration process
Image-acquisition method
Morent, Rino, et al. "Measuring the wicking behavior of textiles by the combination of a horizontal wicking experiment and image processing."Review of scientific instruments 77.9 (2006): 093502.

## Slide 7: Current ways to test the infiltration process
Resistance method
http://www.eytest.com/ey60.html

## Slide 8
Methodology
Fabrics and apparatus design

## Slide 9
Methodology
Fabrics and apparatus design
Mechanism of liquid absorption. Step one, the drop water is absorbed into the fabric. step two, the drop water infiltrates into the fabric through wicking.

## Slide 10
Methodology
Fabrics and apparatus design
specimen | Sample 1 | Sample 2 | Sample 3 | Sample 4 | Sample 5
Fabric content | PET (Polyester) | Cotton &hemp | Hemp | PET& cotton | Cotton
Average thickness(mm) | 0.16 | 0.32 | 0.38 | 0.68 | 0.85
Average weight(g/) | 28.0 | 86.0 | 102.0 | 189.0 | 112.0
specimen | Sample 1 | Sample 2 | Sample 3 | Sample 4 | Sample 5
Fabric content | PET (Polyester) | Cotton &hemp | Hemp | PET& cotton | Cotton
Average thickness(mm) | 0.16 | 0.32 | 0.38 | 0.68 | 0.85
 | 28.0 | 86.0 | 102.0 | 189.0 | 112.0

## Slide 11
Methodology
Experiments
Equipment schematic diagram of the FLTS. a, Working principle diagram. b, The water drop downwardly infiltrates the fabric. c, The water drop laterally infiltrates the fabric.

## Slide 12
Lateral and upward infiltration
Experiments
Downward infiltration
Lateral infiltration
Upward infiltration

## Slide 13
Results and analyses
Downward infiltration
Sample1, Polyester
Sample2, Cotton & hemp

## Slide 14
Results and analyses
Downward infiltration
Sample 3, hemp
Sample 4, Polyester & Cotton

## Slide 15
Results and analyses
Downward infiltration
Sample 5, Cotton
Average infiltration level of each sample

## Slide 16
Results and analyses
Lateral and upward infiltration

## Slide 17
Conclusions
The liquid transfer properties of the fabrics are different, which means that they have different moisture management ability;
Gravity affect the rate of liquid transfer when directions of the infiltration and gravity are different;
The noncontact way is able to evaluate the liquid transfer property of textiles

## Slide 18: Thanks Merry Christmas